Mohr-Coulomb Model

Computational Geotechnics

Contents

Idealized and Real Stress-Strain Behavior of Soils

Basic Concepts of Mohr-Coulomb Model

Mohr-Coulomb Model Modeling

Friction Angle

Influence of Intermediate Principal Stress on Friction Angle

Drained Simple Shear Test

How to Understand 

Drained Triaxial Test

Reference

Appendix A

Appendix B

Idealized and Real Stress-Strain Behavior of Soils

Basic Concepts of Mohr-Coulomb Model

Bilinear approximation of triaxial test

| Basic law: |  | i = x, y, etc. |
| --- | --- | --- |
|  | reversible elastic strain |  |
|  | irreversible plastic strain |  |

for f < 0

f = yield function

Mohr-Coulomb Soil Modeling

Mohr-Coulomb Soil Modeling

| Flow rule for plastic strains: |  |  |  |  |
| --- | --- | --- | --- | --- |
| This means: |  |  | , , etc. |  |
|  | a multiplier that determines the magnitude of plastic strains |  |  |  |
|  |  | determines the direction of plastic strains |  |  |

Classical associated plasticity: g = f

General non-associated plasticity: g  f

M-C model: f  r – s sin – c cos : yield function

g  r – s sin – c cos : plastic potential function

Mohr-Coulomb Soil Modeling

Nonlinear Failure Envelope Representation

Friction Angle Definitions

(Kulhawy and Mayne, 1990)

Strength Envelopes for a Range of Soil Types

(Bishop, A.W., 1966)

versus Relative Density and Unit Weight

(NAVFAC, “Soil Mechanics Design Manual”, DM-7)

Friction Angle

Dilatancy Angle Relationships

(Bolton, M.D., 1986)

in which:

| 1 | = | Correction for particle shape |  |
| --- | --- | --- | --- |
|  |  | 1 = -6o | For high sphericity and subrounded shape |
|  |  | 1 = +2o | For low sphericity and angular shape |
| 2 | = | Correction for particle size (effective size, d10) |  |
|  |  | 2 = -11o | For d10 > 2.0 mm (gravel) |
|  |  | 2 = -9o | For 2.0 > d10 >0.6 mm (coarse sand) |
|  |  | 2 = -4o | For 0.6 > d10 >0.2 mm (medium sand) |
|  |  | 2 = 0 | For 0.2 > d10 >0.06 mm (fine sand) |
| 3 | = | Correction for graduation (uniformity coefficient, Cu) |  |
|  |  | 3 = -2o | For Cu > 2.0 (well-graded) |
|  |  | 3 = -1o | For Cu = 2.0 (medium graded) |
|  |  | 3 = 0 | For Cu < 2.0 (poorly graded) |
| 4 | = | Correction for relative density (Dr) |  |
|  |  | 4 = -1o | For 0 < Dr <0.5 (loose) |
|  |  | 4 = 0 | For 0.5 < Dr < 0.75 (intermediate) |
|  |  | 4 = +4o | For 0.75 < Dr < 1.00 (dense) |
| 5 | = | Correction for type of mineral |  |
|  |  | 5 = 0 | For quartz |
|  |  | 5 = +4o | For feldspar, calcite, chlorite |
|  |  | 5 = +6o | For muscovite mica |
|  |  | (Kulhawy and Mayne, 1990) |  |

cv for NC Clays vs. PI

(Mitchell, 1993)

(Bolton, 1986)

Influence of Intermediate Principal Stress on Friction Angle

| Introduction: Models and soil mechanics | Special conditions; Name of test; Diagram. σa≠σb≠σc; True triaxial. σb=σc=σr; Cylindrical compression The “triaxial” test. εb=0; Plane strain or biaxial. σb=0; Plane stress. εb=εc=εr=0; One-dimensional compression The oedometer test. σb=σc=σr=0; Uniaxial compression or Unconfined compression. σa=σb=σc=0; Isotropic compression. |
| --- | --- |

(Ladd et al., 1977)

Drained Simple Shear Test

How to Understand 

 =  + i or  =  - i

i = inter particle angle of friction

quartz sand:    – 30o

Drained Triaxial Test

| Now |  |  |
| --- | --- | --- |
|  |  | (identical to biaxial test) |

References

Bishop, A.W. (1966), “The Strength of Soils as Engineering Materials”, Geotechnique, Vol. 16, No. 2, pp. 89-130.

Bolton, M.D. (1986), “The Strength and Dilatancy of Sands”, Geotechnique, Vol. 36, No. 1, pp. 65-78.

Duncan, J.M and Buchignani, A.L. (1976), “An Engineering Manual for Settlement Studies”, Report, Department of Civil Engineering, University of California, Berkeley, 94 pages.

Janbu, N. (1963), “Soil Compressibility as Determined by Oedometer and Triaxial Tests”, Proc. 3rd European Conference on Soil Mechanics and Foundation Engineering, Wiesbaden, Germany, Vol. 1, pp. 19-25.

Janbu, N. (1985), “Soil Models in Offshore Engineering”, Geotechnique, Vol. 35, No. 3, pp. 241-281.

Kulhawy, F.H. and Mayne, P.W. (1990), “Manual on Estimating Soil Properties for Foundation Design”, Report EL-6800/1493-6, Electric Power Research Institute.

Ladd, C.C., Foott, R., Ishihara, K., Schlosser, F., and Poulos, H.G. (1977), “Stress-Deformation and Strength Characteristics”, Proc. 9th Int. Conference on Soil Mechanics and Foundation Engineering, Tokyo, Japan, Vol. 2, pp. 421-494.

Mitchell, J.K. (1993), “Fundamentals of Soil Behavior”, John Wiley & Sons, Inc., New York, 2nd Edition.

Naval Facilities Engineering Command, NAVFAC, “Soil Mechanics Design Manual”, DM-7, Alexandria, Virginia, 1982, 355 pages.

Pestana, J. (2001), PLAXIS Lecture Notes, Department of Civil and Environmental Engineering, University of California, Berkeley.

Wroth, C.P. and Wood, D.M. (1978), “The Correlation of Index Properties with Some Basic Engineering Properties of Soils”, Canadian Geotechnical Journal, Vol. 15, No. 2, pp. 137-145.

Appendix A

| Determination of |  | from plasticity theory in drained simple shear test: |
| --- | --- | --- |

| Rate of volume change: |  |  |  |
| --- | --- | --- | --- |
| We will proof: |  |  |  |
| At failure only plastic strains! |  |  |  |
| Hence: |  |  |  |

Appendix B

Drained Biaxial Test

Determination of  in drained biaxial test:

+

Appendix B

Drained Biaxial Test

| Difference with triaxial test: | Plane strain |
| --- | --- |

Appendix B

Drained Biaxial Test