Determination of Soil Stiffness Parameters

Computational Geotechnics

Contents

General concepts and stiffness of sand

Hooke’s law

E-moduli from triaxial testing

E-moduli from oedometer testing

Examples on the estimation of E

Stiffness of clays

Undrained clay behavior

Drained clay behavior

Examples on the estimation of E

Idealized and real stress-strain behavior of soils

Idealized types of stress-strain behaviors: (a) nonlinear elastic model. (b) linear elastic model, and (c) elastoplastic model

Various types of elastoplastic behaviors: (a) strain hardening, (b) perfectly plastic, (c) strain softening, and (d) combination of a to c.

(Bardet, 2000)

Hooke’s Law of Isotropic Elasticity

Standard Drained Triaxial Test on Sand

Oedometer Test on Sand

Oedometer Test on Sand

| Hooke: |  |
| --- | --- |
| Loose: | Epref≈150×23σypref |
| Dense: | Epref≈500×23σypref |

| Loose: | Epref≈150×232σxpref≈150σxpref |
| --- | --- |
| Dense: | Epref≈500×232σxpref≈500σxpref |

This implies:

Summary on Stiffness Parameters: Sand

(Laboratory based experience)

| Loose: |  |
| --- | --- |
| Dense: |  |
| Loose: |  |
| Dense: |  |

Unloading: About 4 times stiffer.  small

Selection of Moduli for FEM-Computation

Examples 1 (loading):

Layer 1 (extremely loose sand):

| Mohr-Coulomb model: |  |  |
| --- | --- | --- |
| Layer 1: |  |  |
| Average: |  |  |

Selection of Moduli for FEM-Computation

Examples 2 (unloading):

| Layer 1 (dense): |  |
| --- | --- |
| Layer 3 (medium): |  |
| Unloading: Eurref≈4E50ref,ν≈0.15for both layers |  |
| Mohr-Coulomb model: |  |
| Layer 1: |  |
| Layer 3: | E=4×300000.10≈38000kPa |

Eoed from Cone Penetration Test in Sands

| Cone Resistance | : |  |  |
| --- | --- | --- | --- |
| Correlation | : |  |  |
| Literature NC-sand | : |  | to 3 |
| Vermeer’s experience | : |  |  |
| Alternatively | : | Eoed=(30±10)qcpref |  |

Undrained Triaxial Test on Clay

| Normally consolidated clay: |  |
| --- | --- |
| Cu = undrained shear strength (or Su) |  |

Idealized and real stress-strain behavior of soils

(Ladd et al., 1977)

Plate Loading Tests by Duncan & Buchignani (1976)

Summary on Stiffness Parameters: Clay

Undrained Conditions

Do not use empirical relationships only.  Get good quality experimental data from lab tests, cone penetration tests and vane tests

Drained Behavior for Clays

Summary on Stiffness Parameters: Clay

Drained Conditions

| For loading: |  |  |
| --- | --- | --- |
| For unloading |  |  |
| NC Clay: | Soft: |  |
|  | Dense: |  |
|  | Soft: |  |
|  | Dense: |  |
| OC Clay: (large variations, be careful) |  |  |
|  | Soft: | Eoedpref=10σc'pref×(2↔5) |
|  | Dense: | Eoedpref=30σc'pref×(2↔5) |
|  | Soft: |  |
|  | Dense: |  |

Relationships Between Elastic Constants